

|  |
| --- |
| **SYSTEM : EPOXY BASED FLOOR COATING** |
| **Floor- LD Indoor** |

**System Description**

**Primary Coat: 1 coat of Floor Guard Epoxy Primer @ 50 μ**

A high performance two pack epoxy primer specially designed to penetrate into, and seal the surface of concrete. Provides sound base for improved adhesion of subsequent Berger epoxy or polyurethane based coatings. This is a part of the anti-carbonation system.

**Volume Solids:** 45% ± 2%

**Secondary Coat: 2 coats of Floor Guard Epoxy @ 50 μ each**

A two pack modified epoxy coating with excellent resistance to abrasion and to fresh and salt water, non oxidizing acids, oils and many other chemicals.

**Volume Solids:** 52% ± 2%

**Designed Use**

Designed for industrial floors, floors of parking areas, traffic areas, walkways, battery rooms and equipment rooms which are subjected to heavy movement. 